## Slide 1: Using Neural Networks to Analyze LIBS Data

## Slide 2: Outline
Introduction
  The data set
Benchmark
Classification
  Patternnet
  Probabilistic Neural Network
Regression
Moving forward

## Slide 3: Introduction

## Slide 4: Introduction
We have a recipe for urban melt glass
Want to measure homogeneity
Further application: handheld LIBS
GOAL: given a LIBS spectrum, determine what quantity of each analyte is present

## Slide 5: What is LIBS?
LASER Induced Breakdown Spectroscopy
Handheld devices
Notes: A short (ns or fs) laser pulse ablates the surface of a sample, forms a plasma. The elements/constituents of this plasma form larger compounds, emitting light as they do. This light is collected and turned into a spectrograph. It depends on laser power and the delay between ablation and collection of the signal

## Slide 6: The Dataset
11 samples
20 spectra per sample
11725 channels
Chart: Base + MgO
Notes: Made 11 Samples
All samples had SiO2 (sand), Fe2O3 (rust), and NaO (to make it stick together)
10 samples had an additional analyte of interest from our urban meltglass
Al2O3, CaO, KOH, MgO, S, BaO, MnO, Ca3(PO4)2, TiO
No Uranium! 
Each sample shot 20 times at slightly different location on puck

## Slide 7: Classify Sample by Analyte
First Task:

## Slide 8: Simple RBF
Average the samples in the training set
Use RBF to measure deviation of each spectrum from this average
Choose the one with the highest value

## Slide 9: Results

## Slide 10: Test set…

## Slide 11: Probabilistic Neural Network
RBF neuron for each training sample

## Slide 12: Optimizing Width
~Global minimum around 80
Local minima around 150 and 450
Resists gradient descent

## Slide 14: Quantify the Constituent Elements
Second Task

## Slide 15: Generalized Regression Neural Network
Lorem
Ipsum
Dolor
Simet

## Slide 16: Optimizing width
Want to avoid overfitting
Cross-validation method

## Slide 17: Comparison with PatternNet
RBF
Error (val): 1.5201
PatternNet
Error (val): 0.0056